SECTION 077253

SNOW BRACKETS/SNOW GUARDS

- – GENERAL

  - SECTION INCLUDES

    - Snow Bracket/Snow Guards.

  - RELATED SECTIONS

    - Section [073200 – Roof Tiles]

  - REFERENCES

    - NRCA Roofing and Waterproofing Manual.

    - WSRCA and TRI Concrete and Clay Tile Roof Design Criteria for Cold and Snow Regions Manual

- – PRODUCTS

  - MANUFACTURERS

    - Acceptable Manufacturer: TRA Snow and Sun, which is located at: 1657 South 580 East; American Fork, UT  84003; Toll Free Tel: 800-606-8980; Tel: 801-756-8666; Email: info@trasnowandsun.com; Web: www.trasnowandsun.com

    - Substitutions: Not Permitted.

  - SNOW BRACKETS/SNOW GUARDS

    - PRODUCT: As manufactured by TRA Snow and Sun.

      - Application: Used on tile roofs.

      - Model: Snow Bracket A (Classic or Apex): Concrete Tile Roof, 16-1/2 inch length (420 mm).

      - Materials: Steel, 16 ga (ASTM A879).

      - Materials: Aluminum .063 inch (H32-ASTM B209).

      - Materials: Copper, 48 oz (ASTM B152).

      - Materials: A606, 16 ga (ASTM A606).

      - Materials: Stainless Steel, 16 ga (ASTM A240).

      - Finish: Powder coated, ______________.

      - Finish: Powder coating color as selected by Architect from TRA Standard colors.

      - Finish: Raw steel.

      - Finish: Electro-galvanized steel.

      - Finish: Hot-dipped galvanized steel.

      - Finish: Mill finish Aluminum.

      - Finish: Mill finish Copper.

      - Finish: Mill finish A606.

- EXECUTION

  - SNOW FENCE INSTALLATION

    - Snow Brackets: Install products in accordance with manufacturer’s installation instructions and engineered layout charts.

      - Bracket Type A: Install on the top surface of the tile with the triangular end of the bracket over the headlap of the tile and the spike into a 1 inch by 2 inch (25 mm x 51 mm) batten.

END OF SECTION